**BEGO Triniq** - Intensity 16, Duty 8, Time 150 + UV-B Block box

**Dentona Lumina** - Intensity 12, Duty 8, Time 150 + UV-B Block box

**Pro3Dure GR 14.1** - Intensity 12, Duty 8, Time 300

**Asiga Denta resins** - Intensity 12, Duty 8, Time 240